## Slide 1
Radek Zbořil
Palacky University
RCPTM, Olomouc
„Our planet's physical, chemical, and biological processes are influenced or driven by the properties of nanoparticles.“ M. F. Hochella, Science, 2008
Nanotechnologies – world of small
dimensions and big opportunities

## Slide 2
1959 – R. Feynmen, APS meeting, Pasadena
„There‘s Plenty of Room at the Bottom” vision of nanonotechnologies
prediction of discovery of memory chip, method of nanomanipulation
1981 – scanning tunneling microscopy (STM)
possibility of 3D imaging with atomic resolution Nobel Prize - Binning, Rohrer - 1986
1965
Nanohistory… When did it start?

## Slide 3
1991 – nanotubes
Nature,1991
S. Iijima
1985 – discovery of fullerene C60
Nobel prize – 1996
Kroto, Smalley, Curl
2004 – discovery of graphene
Nobel prize - 2010
A. Geim, K. Novoselov
0D
1D
2D
3D
Nanohistory … It started with carbon

## Slide 4
in human body
in water
in lower and higher organisms
It started much earlier …
Nano-objects are all around us

## Slide 5
in the atmosphere (volcanic activity, aerosols, wind erosion)
on Mars
It started much earlier …
Nano-objects are all around us
G. Klingelhofer et al. Science 306 (2004) 1740.

## Slide 6
FLUORESCENCE, CHANGE COLOR
QUANTUM dots (CdSe)
SILVER NANOPARTICLES
What nanoparticles can…

## Slide 7
DIAGNOSE
NANOPARTICLES AS CONTRAST AGENTS IN MRI IMAGING
What nanoparticles can…

## Slide 8: Co What nanoparticles can…
TREAT
NANOPARTICLES FOR TARGETED DRUG DELIVERY AND MAGNETIC FLUID HYPERTHERMIA

## Slide 9
IRON NANOPARTICLES IN GROUNDWATER TREATMENT TECHNOLOGIES
What nanoparticles can…
PURIFY

## Slide 10
STORE
HARD DISCS BASED ON MAGNETIC NANOPARTICLES
NANOCARBON FOR HYDROGEN STORAGE
MRAM MEMORIES (spintronics, magnetoelectronics)
What nanoparticles can…

## Slide 11
PROTECT
CARBON NANOTUBE BASED
SUPERHYDROPHOBIC COATINGS
What nanoparticles can……
INSPIRATION IN NATURE
(LOTOS LEAF)

## Slide 12
LOVE
What nanoparticles can……

## Slide 13
Name SURNAME
xxxxxxxxxxxxxxxxxxxxxxxxxx
Nanotechnologies in/from Olomouc
2011
+ 2013
2010-2014 ESF support by Operational Program Research and Development for Innovations (25 mil. Euro, 100 scientists in 2014)

## Slide 14
Name SURNAME
xxxxxxxxxxxxxxxxxxxxxxxxxx
Distinguished and visiting scientists, collaborators
Prof. P. Hobza
RCPTM
H-index: 78
 21 000 citations
non-covalent interactions
Prof. A. Gedanken
Bar Ilan University, Israel
H-index: 65
 15 000 citations
contract from January 2012
Nanometals, sonochemistry
Prof. R. Varma,
US Environmental Protection Agency,
H-index: 60
 12000 citations
Green chemistry, nanotoxicity
Prof. E. P. Giannelis
Cornell University
H-index: 52
18 000 citations
carbogenic quantum dots
Prof. M. Gratzel
EPFL Lausanne
H-index: 140
93 000 citations
iron oxide films
Prof. S. Ohkoshi
University of Tokyo
H-index: 46
7000 citations
magnetic nanoparticles

## Slide 15
Iron based nanomaterials…
Iron age in nanotechnologies
targeted drug delivery
cell labeling and separation
magnetic fluid hyperthermia
MRI contrast enhancement
water treatment technologies
heterogeneous catalysis
dye-sensitized solar cells
M. Hermanek, R. Zboril et al.
J. Am. Chem. Soc.
129, 10929, 2007.
Bakandritsos et al. SMALL 8, 2381, 2012; ADV. FUNCT. MATER. 18, 1694, 2008; NANOSCALE 2, 564, 2010.
K. Sivula, R. Zboril et al.
J. Am. Chem. Soc. 132, 7436, 2010; I. Cesar, JPC-C 113, 772, 2009.

## Slide 16
Iron oxide based nanomaterials – synthetic approach
20 nm
FeO
-Fe
-Fe
FeOOH
Hydrogen furnace
Fe
+ N2
+ H2O
+ N2(2%O2)
air
-FeO(OH)
+ H2
-Fe2O3
Fe/FeO

## Slide 17
Nanoscale zero valent iron (nZVI) for water treatment technologies
Slurry feeding during treatment. © Aquatest, Czech Republic
Remediation in Pisecna © Aquatest, CZ
The first European producer of nZVI in a large scale. Pilot and full-scale remediation at various localities in Europe and US.
(e.g. AQUATEST, CZ; AECOM, USA, GEO LAB USA)
J. Filip, R. Zboril et al. EST. 41, 4367 (2007).
R. Zboril et al.: PCT/CZ2008/000040
nZVI – environmentally friendly reduction technology of treatment of ground water.
Applicable for removal of more than 70 pollutants, e.g. chlorinated hydrocarbons arsenic, uranium, chromium, heavy metals, herbicides, nitrobenzen and nitro-derivatives, dioxine, PCB, phosphates etc.

## Slide 18
Nanoscale zero valent iron (nZVI) for water treatment technologies
Decrease of chlorinated ethenes after 1 year from injection of nZVI (locality Pisečná, CZ, 2010); remediated by AQUATEST
Treatment of Cr(VI)
KARA Trutnov,CZ, 2011; remediated by: ECORA
Chart: 
| 8.9. | 20.9. | 22.10.
cis-1,2 -dichlorethene | 2340 | 1060 | 31
tetrachlorethene | 903 | 62.6 | 37.7
vinylchloride | 278 | 70.4 | 40
Chart: 
| 8.9. | 20.9. | 22.10.
C [mg/l] | 42.2 | 0.5 | 0.5
Treatment of chlorinated ethenes
KARA Trutnov,CZ, 2011; remediated by ECORA
C
[mg/L]
C
[µg/L]

## Slide 19
Nanoiron in the fight with cyanobacteria
B. Maršálek et al. EST 46, 2316, 2012; R. Zbořil et. al. PCT/CZ2011/0075
High and selective toxicity against cyanobacteria
Toxicity against daphnia, water plants and fishes is 2-3 orders of magnitude lower!
Cell
destruction
Original cells
Deformation of cells

## Slide 20
Nanoiron as a multipronged weapon against cyanobacteria
4 modes of action:
Preventive mode – removal of bioavailable phosphorus.
Destructive mode – cell destruction
Immobilization mode – ability to immobilize microcystin on the large and positively charged surface of the non-toxic and environmentally benign ferric hydroxide
Physical mode - formation of a highly flocculated waste product consisting of destroyed biomass
and Fe(OH)3
In spite of the cell destruction, microcystin is not released in the water column!
B. Maršálek et al. EST 46, 2316, 2012; R. Zbořil et. al. PCT/CZ2011/0075.
ccommercial herbicide
Before
After nZVI treatment

## Slide 21
Nanoferrates (IV,V,VI) for advanced water treatment
Reactor for ferrates application working in nitrogen atmosphere
Control and measurement of pH, ORP, temperature, dosage
- High efficiency of removal of e.g. aromatic compounds, cyanides, heavy metals, chemical warfare agents, arsenic
Collaboration with ASIO; Patent application
R. Zboril et al. J. Hazard. Mater. 211, 126, 2012.
J. Filip et al. Chem. – Eur. J. 17, 10097, 2011;
.
Environmentally friendly in-situ applicable technology;
magnetically separable product; arsenic embedded in crystal lattice

## Slide 22
Magnetic Iron oxide nanoparticles for MRI imaging
K. Kluchova, R. Zboril et al. Biomaterials 30, 2855, 2009.
M. Maslan et al. Patent No. 300445 Accepted 9. 4. 2009.
-Fe2O3/bentonite
Lumirem
a one-step thermal decomposition of iron(II) acetate in air at 400 °C  nearly monodispersed superparamagnetic maghemite nanoparticles
-Fe2O3
After disperison in bentonite matrix  highly effective and cheap peroral MRI negative contrast agent for gastrointestinal tract
gall stone
-Fe2O3/bentonite
small bowel
2010-2011: clinical trials with more than 100 patients (FN Olomouc, Banska Bystrica)
negotiation on the license conditions – MEDIHOPE, GML Health Care
extraluminal metastases

## Slide 23
Iron oxide films for direct solar splitting of water
K. Sivula, R. Zboril et al. J. Am. Chem. Soc. 132 (2010) 7436-7444.
Mesoporous hematite prepared by a solution-based colloidal approach  a drastic effect of sintering temperature on the photoactivity effieciency due to Sn doping

## Slide 24
More on iron oxide nanoparticles
L. Machala, J. Tuček, R. Zboril: Polymorphous transformation of nanometric iron(III) oxide: A review, Chem. Mater. 23 (2011) 3255-3272.
J. Tucek, R. Zboril, A. Namai, S. Ohkoshi, Chem. Mater. 22 (2010) 6483-6505.
L. Machala, R. Zboril, A. Gedanken: Amorphous iron(III) oxide – a review, J. Phys. Chem. B 111 (2007) 4003-4018.
R. Zboril, M. Mashlan, D. Petridis: Iron(III) oxides from thermal processes - synthesis, structural and magnetic properties, Mössbauer spectroscopy characterization, and applications, Chem. Mater. 14 (2002) 969-982.

## Slide 25
Synthesis and functionalization of Ag NPs
Immobilization of NPs on solid substrates
Antibacterial, antifungal activity, cytotoxicity
Medical and disinfection applications
Nanosilver - new chance in fight with bacteria and fungi?
25 nm 200 nm 400 nm
Drastic effect of particle size on antibacterial activity
A. Panáček et al. J. Phys. Chem. B. 110 (2006) 16248; more than 350 citations.
Candida spp.
A. Panacek al. Biomaterials 30 (2009) 6333-6340.
Antifungal activity even higher compared to commercial fungicides

## Slide 26
Toxicity of nanosilver against eukaryotes and higher organisms
Paramecium caudatum
1 h LC50 = 39 mg·L-1
 10x lower toxicity compared to bacteria, yeasts and fungi
L. Kvitek et al JPC- C 113 (2009) 4296;
A. Panacek al. Biomaterials 30 (2009) 6333.
Ag NPs ~25 nm
Drosophila melanogaster
A. Panacek et al. EST 45 (2011) 4974.
Acute toxicity  20 mg/L
Cytotoxicity to human fibroblasts
Ag0
Ag+
LC50(Ag0) ~ 30 mg/L
LC50(Ag+) ~ 1 mg/L

## Slide 27
Covalent immobilization of nanoAg –
new generation of antimicrobial coatings
Z. Markova et al. Green Chem. 14, 2550, 2012. R. Prucek et al. Biomaterials 32, 4704, 2011; Dallas et al. Adv. Funct. Mater. 20, 2347, 2010.
Polymer acts simultaneously as a reducing agent and substrate for covalent immobilization of nanoAg – no release to environment, no need of extra reducing agent!
P. Dallas et al Macromol. Mater. Eng. 295, 108, 2010.
Covalent antimicrobial modification of textile fibers and filtration membranes – MEGA, a.s.
Reusable antimicrobial
dispersions

## Slide 28
NanoAg antimicrobial coatings for medical applications
NanoAg-PEI coating of tracheostomy cannulas;
Stage of clinical trials (UVN Prague, KARIM); negotiation on the license conditions (Biomedica, s.r.o.)
R. Zbořil, J. Soukupová, Patent No. 303502, accepted 12. 9. 2012; PCT/CZ2012/000068.
Challenge:
NanoAg induced activation of ATB against resistant bacterial strains;
in vitro testing completed; stage of in vivo trials with animal models
Modification of surgical thread

## Slide 29
More on nanosilver…
P. Dallas, VK Sharma, R. Zboril Adv. Colloid Interface Sci 166 (2011) 119.
Suggested mechanisms of antimicrobial action
Synthetic approaches towards silver nanocomposites
Thin films, covalent immobilization
Applications

## Slide 30
Carbon nanostructures
perfluoro-alkylsilan
0.6 nm
5 nm
Chem. Mater. 20 (2008) 2884;
Chem. Mater. 20 (2008) 4539.
Small 4 (2008) 455.
Small 5 (2009) 1841.
Chem. Commun.46 (2010) 1766.
Small 6 (2010) 2885.
Chem. Mater 24 (2012) 6.
J. Mater. Chem. 22 (2012) 16219.
2D graphene,
synthesis,
derivatives,
functionalization
1D nanotubes,
functionalizationapplications
OD carbon dots,
synthesis,
functionalizationapplications

## Slide 31
Carbon based quantum dots
5 nm
Bourlinos et al. Chem. Mater. 20 (2008) 4539; Small 4 (2008) 455; Chem. Mater 24 (2012) 6; Krysman et al. JACS 134 (2012) 747.
Ferromagnetism of CDs!
Srivastava et al. ChemPhysChem 12 (2011) 2624.
Advantages compared to common (CdSe) QDs:
Large scale production
Biocompatible nature, low toxicity (CHNO)
Surface functionalized » possibility to bind other species » multifunctional hybrids
Two sources of fluorescence: carbon core, organic surface layer
Magnetic properties
Various surface
functionalities
Thermally induced solid-state syntheses starting from organic precursors (citrate, betaine etc.)

## Slide 32
Carbon nanocomposites and their applications
rat mesenchymal stem cell labeling
dual MRI/fluorescence probes
advanced sorption-reduction water treatment technologies - GEOTEST
Magnetic Fe3O4/C-dots
Nanocarbon/iron composites
CMK-3 carbon
Gd doped C-dots
Z. Markova et al. J. Mater. Chem. 22 (2012) 16219;
AB Bourlinos et al. J. Mater. Chem. 2012, in print.
T1-weighted images
T1-MRI
T2-MRI
M. Baikousi et al. Langmuir 28 (2012) 3918.

## Slide 33
Graphene – synthesis, organic functionalization, interactions with metals
Chemical exfoliation of graphite by perfluorinated aromatic molecules or pyridine as solvents.
graphite in pyridine
Organic functionalization
1 h
5 days
1,3 dipolar cycloaddition of azomethine ylide. Graphene-OH sheets are easily dispersible in polar organic solvents and water.
Small 5 (2009) 1841; Chem. Commun.46 (2010) 1766; J. Phys. Chem. C 116 (2012) 14151.
graphite in benzene
Synthesis
Interactions with metals

## Slide 34
Fluorographene - world's thinnest insulator
Liquid phase exfoliation of graphite fluoride (CF) with sulfolane.
Zboril et al. Small 6 (2010) 2885.
Nair et al. Small 6 (2010) 2877.
First stoichiometric graphene derivative.
The world's thinnest insulator (~3 eV).
Stability higher compared to CH, CCl, CBr.
C3F2Br
band gap  1eV
Suggestion of 2D semiconductors
C2FCl
Band gap engineering in graphene halides
Karlicky et al. J. Chem. Phys 137 (2012) 34709.

## Slide 35
More on graphene
V. Georgakilas, Chem. Rev., DOI: 10.1021/cr3000412, 2012.
Covalent and non-covalent functionalization
Derivatives
Applications

## Slide 36
Acknowledgements
Academic partners:
Colleagues from RCPTM; AB Bourlinos, M. Karakassides (University of Ioannina, Greece, carbon hybrids); EP. Giannelis, M. Krysman, P. Dallas (Cornell University, carbon dots); S. Ohkoshi (University of Tokyo, magnetic nanoparticles); V. Georgakilas (NCSR Demokritos, Athens, graphene functionalization); VK Sharma (Florida Institute of Technology, ferrate technologies); K. Sivula, M. Gratzel (EPFL Lausanne, solar splitting of water); A. Gedanken (Bar-Ilan University, Israel, antimicrobial NPs); KS Kim (Pohang Institute of Technology, Korea, graphene applications); R. Varma (US EPA, toxicity of NPs, nanocatalysis); P. Mulvaney (University of Melbourne, Australia, quantum dots); F. Vianello (University of Padua, biosensors)
Commercial partners:
AECOM US, GEOLAB US, DEKONTA, AQUATEST, GEOTEST, MEGA, AECOM CZ, ECORA (water treatment technologies, pilot testing, full scale remediation)
MEDIHOPE, BIOMEDICA, GML HEALTH CARE, FN Olomouc, UVN Prague, FN Banska Bystrica (antimicrobial treatment, medical applications, in vivo testing)
Grant support:
ESF/MŠMT: 2010-2015: CZ.1.05/2.1.00/03.0058: „Regional Centre of Advanced Technologies and Materials“
NANOREM - (309517 FP7-NMP-LARGE-6) „Taking Nanotechnological Remediation Processes from Lab Scale to End User Applications for the Restoration of a Clean Environment“
TAČR: 2012-2019: TE01020218 Centre of competence: „Environmentally friendly nanotechnologies and biotechnologies for water and soil treatment“
GAČR: 2012-2018: P208/12/G016: Centre of Excellence "Controlling structure and function of biomolecules at the molecular level: theory meets experiment“